INFORMATION ON DOCTORAL THESIS

1. Full name: Nguyen Manh Hung			2. Sex: Male

3. Date of birth: 15/07/1986				4. Place of birth: Phu Tho

5. Admission decision number: No. 4761/QD-KHTN-CTSV, December 29th, 2011 signed by Rector of VNU University of Science.

6. Changes in academic process: Extending document No. 743/QD-DHKHTN, March 3rd, 2016 signed by Rector of VNU University of Science.

7. Official thesis title: “Synthesis and application of sublimable complexes to depositing Cu2O, ZnO thin film by CVD method”

8. Major: Inorganic Chemistry				9. Code: 62440113

10. Supervisors: 	Main supervisor: Prof. Dr. Trieu Thi Nguyet

Co - supervisor:   Ass. Prof. Dr. Nguyen Hung Huy

11. Summary of the new findings of the thesis:

- Successfully fabricated and investigated the effects of deposition temperature, thin film thickness on structural, optical and electrical properties of:

- Cu2O thin films on glass substrates by CVD method from copper(II) pivalate precursor with reacting agent of water vapor.

- ZnO thin films on glass substrates by CVD method from zinc(II) pivalate precursor with reacting agent of water vapor.

- Cu2O/ZnO thin films on glass substrates by CVD method from copper(II) acetylacetonate and zinc(II) pivalate precursors with reacting agent of water vapor.

In which, there has not been any publications about Cu2O and ZnO thin films deposited from their corresponding metal(II) pivalate complexes.

- The applicability of Cu2O/ZnO thin films as a p-n heterojunction in solar cell was characterized. I-V characteristics in dark of the solar cells are non-linear that confirm the formation of the p-n heterojunction. The solar cell characterization under the illumination of 906 W/m2 show that the best solar cell has structure of Au/Cu2O/ZnO(550)/ITO with VOC = 2,0×10-3 V, ISC = 3,9×10-8 A, filling factor of FF = 23.43×103 and efficiency of η = 6,47×10-2 %.

- The applicability of ZnO thin films deposited on ITO/glass substrate in gas sensor was characterized. The obtained results show that the sensor made using ZnO thin film deposited at 550oC from zinc(II) pivalate has high selectivity to NO2 and can work well at room temperature with quite short response and recovery times.

12. Practical applicability, if any: Applicability in fabricating devices: gas sensor, solar cell, thin film transistor, etc.

13. Further research directions, if any: Study the application of metal oxide thin films deposited by CVD method in manufacturing solar cell, gas sensor, thin film transistor, optical device.

14. Thesis-related publications:

[1] Nguyen Thi Lua, Trieu Thi Nguyet, Nguyen Manh Hung, Nguyen Hung Huy (2012), “Effects of temperature on phase composition and properties of Cu2O thin film deposited by CVD method from copper(II) acetylacetonate with H2O-H2O2 vapor”, Vietnam Journal of Chemistry 50(5B), pp. 283-287.

[2] Nguyen Thi Lua, Trieu Thi Nguyet, Nguyen Manh Hung, Nguyen Hung Huy (2012), “Effects of temperature on phase composition and properties of Cu2O thin film deposited by CVD method from copper(II) acetylacetonate with water vapor”, Vietnam Journal of Chemistry 50(5B), pp. 288-292.

[3] Trieu Thi Nguyet, Nguyen Thi Lua, Nguyen Manh Hung, Nguyen Hung Huy (2012), “Effects of temperature on the phase composition and physcial properties of Cu2O thin film deposited by CVD method from copper(II) acetylacetonate precursor with reacting agent of ethanol-water vapor”, Journal of Analytical Science 17(4), pp. 3-7.

[4] Nguyen Manh Hung, Trieu Thi Nguyet, Nguyen Hoang Le, Nguyen Hung Huy (2013), “Effects of temperature on structural and optical properties of ZnO thin films deposited by CVD method from zinc pivalate precursor”, Vietnam Journal of Chemistry 51(3AB), pp. 320-323.

[5] Trieu Thị Nguyet, Nguyen Thi Lua, Nguyen Manh Hung, Nguyen Hung Huy (2013), “Effects of reaction agents on Cu2O thin film deposited by CVD method from copper(II) acetylacetonate”, Journal of Analytical Science 18(1), pp. 74-78.

[6] Nguyen Manh Hung, Trieu Thi Nguyet, Nguyen Hung Huy (2013), “Effects of temperature on structural and electrical properties of ZnO thin film deposited by CVD method from zinc pivalate precursor”, Vietnam Journal of Chemistry 51(6ABC), pp. 216-219.

[7] Nguyen Manh Hung, Trieu Thi Nguyet, Nguyen Hung Huy, Nguyen Hoang Le (2013), “Effects of temperature on structural and optical properties of Cu2O thin film on ZnO/glass substrate deposited by CVD method from copper(II) acetylacetonate precursor”, Vietnam Journal of Chemistry 51(6ABC), pp. 220-224.

[8] Nguyen Manh Hung, Trieu Thi Nguyet, Nguyen Hung Huy, Pham Anh Son (2015), “Effects of temperature on structural, optical and electronic properties of Cu2O thin film deposited by CVD method from Cu(II) acetylacetonate precursor”,  Journal of Analytical Science 20(1), pp. 74-79.

[9] Nguyen Manh Hung, Trieu Thi Nguyet, Nguyen Hung Huy, Pham Anh Son (2015), “Effects of temperature on structural and optical properties of ZnO thin film deposited by CVD method from zinc pivalate precursor”, Journal of Analytical Science 20(2), pp. 64-69.

[10] Nguyen Manh Hung, Trieu Thi Nguyet, Nguyen Hung Huy, Nguyen Thanh Tho (2015), “Effects of thickness on structural and electrical properties of Cu2O thin film”, Vietnam Journal of Chemistry 53(3e12), pp.119-122.

[11] Nguyen Manh Hung, Trieu Thi Nguyet, Nguyen Hung Huy, Dang Xuan Chat (2015), “Effects of thickness on structural and electrical properties of ZnO thin film”, Vietnam Journal of Chemistry 53(3e12), pp.123-127.